## Slide 1
Cavity expansion and nanohybrid copper phytate @ halloysite coated with polyphosphazene for reducing smoke release and fire hazard of epoxy resin
Abstract
In the present work, cavity expansion of HNTs was achieved by etching with sulfuric acid to improve its loading capacity. Then, copper phytate was synthesized and encapsulated in the HNTs to obtain Phyt-Cu@ HNTs. Finally, a sulfonyldiphenol-containing polyphosphazene derivative (PZS) was polymerized and wrapped on Phyt-Cu@ HNTs external surface to form a hierarchical nanohybrid structure (Phyt-Cu@HNTs@PZS). The flame retardancy and smoke suppression of the corresponding EP nanocomposites were significantly enhanced due to the synergistic effect of Phyt-Cu@HNTs@PZS. After adding 5 wt% Phyt-Cu@HNTs@PZS, the peak heat release rate and smoke release rate were reduced maximally by 34.3% and 42.1%, respectively.
7th International Symposium on Fire-Retardant on Fire-Retardant Materials & Technologies
Yuanmeng Lou, Haiyun Ma*, Yanyue Su, Yiheng Ma, Le Yang, Jianzhong Xu*
College of Chemistry and Environmental Science, Hebei University, Baoding 071002, China
Introduction
A novel nanohybrid HNTs-based flame retardant was prepared after a successive cavity expansion, copper phytate encapsulation and polyphosphazene wrapping is named Phyt-Cu@HNTs@PZS and then applied in EP.
Methods
The synthesis of Phyt-Cu@HNTs@PZS (Fig.1)
Fig. 1. Synthesis route of Phyt-Cu@HNTs@PZS
Result
Fig. 2. The analysis of flame retardant
The analysis of FTIR、XRD、XPS demonstrating that we have successfully modified of HNTs
Reference
Fig. 5. Proposed flame retardant mechanism of Phyt-Cu@HNTs@PZS.
Flame retardant mechanism
With the addition of 5% Phyt-Cu@HNTs@PZS, the PHRR and TSP value were decreased, which were 34% and 37.75% compared with EP (Fig. 3). The Raman spectrometer was used to analyze the structural defects of crystals in chars[1]. The results (Fig. 4) show that the ID/IG values of EP nanocomposites higher than that of EP.
During the combustion process, Phyt-Cu, HNTs and PZS play multifunctional roles in both the gaseous phase and condensed phase flame retardant mechanism and finally achieve a comprehensive synergistic flame retardant effect (Fig. 5).
Cavity expansion of HNTs was dispersed in 100 mL of 2 M sulfuric acid
Phyt-Cu@HNTs prepared at 78 ◦C for 2 h
Phyt-Cu@HNTs prepared at 40 ◦C for 4.5 h
EP nanocomposites prepared by melt blinding
Zhao X, Wei P, Qian Y, Yu H, Liu J. Effect of talc on thermal stability and flame retardancy of polycarbonate/PSBPBP composite [J]. Journal of Applied Polymer Science. 2012, 125, 3167–3174.
Fig. 3. HRR、TSP、SPR and COP curves of EP and EP nanocomposites
Fig. 4. Raman spectra of char residual of EP and EP nanocomposites